Fibre Properties

Ginning:

The process of separating the seed from the cotton fiber is called ginning. The ideal ginning is the separation without any damage of the fiber.

Lint and Linters: Raw cotton after ginning is called lint. Or

Cotton fiber after separated from the seed is called lint.

The short, fuzzy fibers still attached to the seed after ginning is called linters.

Importance of raw cotton:

- a. Raw materials represents about 50-75% of the manufacturing cost of a short-staple yarn. This fact alone is sufficient to indicate the significance of the raw material for the yarn producer.

- b. Raw material accounts for about 80% to 90% of the yarn quality.

Brand name of cotton fiber:

- Brand name				Country

- Pima					USA

- Arizona				USA

- SJV					USA

- Elena					CIS

- Parvee					CIS

- Ronda					CIS

- Raja					CIS

- Giza					Egypt

- Andy					Australlia

- Suvin					India

- Delta				            Bangladesh

- Barakat		                        Sudan

CIS: Commonwealth of Independent states (CIS) is the international organization or alliance consisting of eleven former soviet republics Armenia, Azerbaijar, Belarus, Georgia, Kazakhstan, Kyrgyzstan, Moldova, Russia, Tajikistan, Ukraine & Uzbekistan.

Cotton fibers characteristics consider for spinning process:

- 1. Length

- 2. Strength

- 3. Fineness

- 4. Maturity

- 5. Cleanliness

- 6. Color

- 7. Elongation

Elongation: It is a very important for spinning. Without this fiber could not be spinned. Elongation of cotton 6-10%

Elongation is a measurement of the elastic behavior of the fibers in the bundle. The fibers clamped on the bundle with a 1/8 inch distance between the clamps. The first pair of clamps stationary & the back pair of clamps is pulled away at a constant rate. The distance the fibers extend before they break is recorded & expressed as percent elongation.

A table describing ranges of actual elongation values in cotton fibers:

- Elongation			Description

Less than 5.0			Very low

- 5.0 to 5.8			Low

- 5.9 to 6.7			Medium

- 6.8 to 7.6			High

- 7.7 & higher			Very high

Color: The color of cotton is determined by the degree of reflectance (Rd) and yellowness (+b) in the HVI instrument

Reflectance (Rd):

This value expresses the whiteness of the light that is reflected by the cotton fibers.

Yellowness (+b):

This value expresses the Yellowness of the light that is reflected by the cotton fibers.

Importance of color:

As the color of cotton deteriorates due to environmental conditions, the probability for reduced processing efficiency is increased. Color deterioration also affects the ability of fibers to absorb & hold dyes & finishes.

Cotton Grading:

HVI (High Volume Instrument) color grades for American Upland cotton

White

- Color grades		           Symbol		          Code

- Good Middling		GM		            11

- Strict Middling		SM                               21

- Middling			Mid			 31

- Strict Low Middling	            SLM			 41

- Low Middling		            LM			 51

- Strict Good ordinary              SGO			 61

- Good ordinary		           GO			 71

Light Spotted

- Color grades		            Symbol		            Code

- Good Middling		GMLtsp		              12

- Strict Middling		SMLtsp                                     22

- Middling			MidLtsp			 32

- Strict Low Middling	            SLMLtsp			 42

- Low Middling		            LMLtsp			 52

- Strict Good ordinary	            SGOLtsp			 62

Spotted

- Color grades		              Symbol		            Code

- Good Middling		GMLtsp		             13

- Strict Middling		SMLtsp                                     23

- Middling			MidLtsp			 33

- Strict Low Middling      	SLMLtsp			 43

- Low Middling		            LMLtsp			 53

- Strict Good ordinary	            SGOLtsp			 63

- Good ordinary		            GOLtsp			73

Tinged

- Color grades			Symbol		         Code

- Strict Middling		SMLTg                                   24

- Middling			MidTg			           34

- Strict Low Middling		SLMTg                                   44

- Low Middling			LMTg			           55

- Strict Good ordinary		SGOTg		           66

Yellow stained

- Color grades		            Symbol	 	       Code

- Strict Middling		SMYs               	         25

- Middling			MidYs              	         35

Cleanliness & trash content:

Generally many types of foreign matter may contain in cotton stock

Vegetable matter

1. Husk portion

2. Seed fragments

3. Stem fragments

4. Leaf fragments

5. Wood fragments

Mineral matter

- Soil

- Sand

- Dust

Other foreign matters

- Metal fragments

- Cloth fragments

- Packing fragments (mostly polymer)

As spinning process is sensitive to impurities so the fiber should be maintained clean as far as possible. The reason for fiber continuing such foreign matters are:

- Modern high performance plucking system

- Hard ginning, cleaning & pre-drying.

- Careless handling during transportation & packing.

Problem due to unclean fiber:

- Metal parts cut the fibers & harmful to spinning machine.

- Vegetable matter makes disturbance in drafting.

- Vegetable matter jam the carding pin carding machine

- Mineral matter decays the rolling parts of machine.

The scale below represents the degree of contamination:

Up to 1.2%             Very clean

1.2% – 2.0%           Clean

2.0 % - 4.0 %          Medium

4.0 % - 7.0 %          Dirty

7.0% - Above          Very dirty

Fineness:

Fineness is one of the most important fiber characteristics. It determines how many fibers are present in the X-section of a yarn of given thickness.

Micronaire Value of cotton:

The average weight of one inch length of fiber, expressed in micrograms (0.000001g), is called micronaire value of cotton and it is defined by ASTM (American Society for Testing and Materials)

The fineness scale is as follows:

Mic-value			Fineness

Up to 3.1			Very fine

3.1 to 3.9			Fine

4.0 to 4.9			Medium

5.0 to 5.9		            Slightly Coarse

Above 6		            Coarse

Fiber fineness influences primarily:

- Spinning limit

- Yarn strength

- Yarn evenness

- Yarn fullness

- Drape of the fabric product

- Lustre

- Handle

- Productivity of the process

Fiber length:

Fiber length is also one of the most important fiber characteristics. It influences:

- Spinning limit

- Yarn strength

- Yarn evenness

- Drape of the fabric product

- Lustre of the product

- Handle of the product

- Productivity

Different staple length of cotton:

Length class                        		  Length (mm)

Short staple (S)                     	 	   <20

Medium staple (M) 			20.6-25.4

Medium long staple (ML)   		26.2-27.8

Long staple (L) 			28.6-33.3

Extra long staple (XL)		 > 34.9

Fiber Strength:

The bundle strength is the breaking strength of the cotton fibers in grams per tex. The fineness is calculated from the micronaire value. The fiber beard is broken at a continuous deformation rate (constant rate of extension) & with a 1/8 inch distance between the clams.

Strength (grams/tex)				Description

Less than 21					Very weak

22 to 24					Weak

25 to 27					Medium

28 to 30					Strong

31 & higher					Very strong

Fibre Maturity:

Fiber maturity means the thickness of cell wall. The more thick the more mature.

Unripe fibers have neither adequate strength nor adequate longitudinal stiffness. They therefore lead to:

- Loss of yarn strength

- Neppiness

- A high proportion of short fibers

- Varying dye ability &

- Processing difficulties mainly at the card

Maturity may be expressed as the ratio of the actual cross-sectional area of the wall to the area of the circle with the same perimeter.

Maturity Index				Description

Below 0.75					Uncommon

0.75 to 0.85					Immature

0.86 to 0.95					Mature

Above 0.95					Very mature

Bale Management:

Bale management refers to the process of inventory control & selection of fiber according to its properties to maintain homogeneous mixing quality for getting consistent production & quality of yarn. For bale management, all bale samples are tested and bale with almost similar category are arranged for homogeneous mixing.

Object of Bale management:

  - To get uniform yarn quality (consistant).

  - To minimize shade variation of the finished fabric.

  - To reduce fabric ‘barre.’

Factors consider for efficient Bale Management system:

- Origin (Country of origin)

- Length & Length uniformity

- Fineness

- Strength & elongation

- SCI (Spinning consistency index)

- Maturity

- Color

- Trash%, etc.

Bale management procedure:

1. At first 100% bales of a lot are tested. Normally Micronaire value and color grade are taken as parameter to be tested.

| Sl. No. | Bale no. | Mic. | Color grade |
| --- | --- | --- | --- |
| 1 | 1 | 4.0 | GM |
| 2 | 2 | 4.2 | SM |
| 3 | 3 | 4.1 | GSM |
| - | --- |  | ---- |
| 1200 | 1200 | 4.0 | SM |

2. After that closely similar Mic (+ 0.3) and color grades bales are selected.

| Mic. | Color grade |  |  | Total |
| --- | --- | --- | --- | --- |
|  | GM | SM (S) | SM |  |
| 3.9 | 75 | 25 | 4 | 100 |
| 4.0 | 90 | 8 | 2 | 104 |
| 4.9 | 110 | 20 | 5 | 135 |

- Then the Micronaires  which have the major proportion in the lot are taken.

- Finally a number of bales are selected according to the capacity of the industry.

Let,

Total no. of bale: 800

Daily consumption: 40 bales

No. of days to process the lot: 800/40 = 20.

SCI: Spinning consistency Index is a calculation for predicting the spin ability of the fibers. A multiple regression equation can provide valuable information to anticipate the yarn strength and spinning potential. The regression equation uses most of the individual HVI measurement results to calculate the SCI. This index can be used to simply the category system used in the cotton warehouse. In general, the higher the index, the higher the yarn strength and the better the overall fiber spin ability.

The equation for the SCI value is:

Spinning consistency index (SCI) = -414.67+2.9 x Strength – 9.32 x Micronaire + 49.17 x Length (inch) + 4.74 x Uniformity + 0.65 x Rd + 0.36 x (+b)