## Slide 1: Garments Testing
Objectives:
To assure the quality of apparel.
To satisfy a customer.
Essential testing for apparels-
1. Shrinkage test T-shirt > knit garments
2. GSM test
3. Color fastness test
4. Fiber composition Woven + knit
5. Color shade etc.

## Slide 2: Description of Five Essential Tests
a) Color shade: Visual appearance of sample.
Requirements:
1. Light box
2. Approved sample
3. Garments sample
Procedure:
1. At first we should placed the sample inside light box.
2. Approved sample placed on the side of first sample.
3. Then we have to visually compare the color shade.
4. Make comments either it is accepted or not accept.

## Slide 3: Continued……
b) Color fastness:
Requirements:
1. Sample preparation
* Washing m/c
* Dryer
* Conditioning, 24 hrs in standard testing lab.
2. Test
To do this we need
* Light box
* Grey scale
* Sample (Before wash)

## Slide 4: Continued……
3. Procedure
* Before wash sample and after wash sample placed side by inside light box.
* Compare between this two and rating by grey scale.
4. Evaluation:
If rating is 5, it means excellent (no change of color)
If the rating is 4, it means very good for 3 it is good, for 2 it is Fair and for 1 it is Poor.
N.B: Color fastness to light rating 1-8. Blue scale is used for assessment.

## Slide 5: Continued……
c) GSM
Requirements:
1. GSM cutter.
2. Rubber board
3. Digital balance
Procedure:
Placed the sample on rubber board.
Put the GSM cutter on the fabric.
Press and rotate the GSM cutter to cut fabric.
Weight the cut sample on digital balance.
d) Fiber composition
1. Burning test
2. Chemical test

## Slide 6: Continued……
d) Shrinkage test: For knit fabric up to 5% shrinkage is internationally accepted and up to 3% shrinkage is internationally accepted for woven fabric.
Requirements: Washing m/c, Dryer, Template, Permanent marker, Scale / measuring tape
Procedure:
Wash the garments / sample according to international standard. Such as ISO, AATCC, BS, etc.
Find out the difference between before wash and after wash sample.
Calculate shrinkage percentage by using below formula.
S% = (LB – LA / LB )* 100
Where, S = Shrinkage, LB = before wash length, LA = after wash length.

## Slide 7
Requirements of Buyers

## Slide 8: Required approvals from buyer
Physical test properties of the fabric
Sample fabric approval
Lab dip approval
Bulk fabric approval
Color continuity approval
Product approval
Grades approval
Pre production sample
Accessories approval for color fastness and quality
During production sample
Folding / packing accessories and method approval