## Slide 1: Swelling Properties
Chapter 06

## Slide 2: Lecture 01

## Slide 3: Swelling Properties of Textile Fibres
When textile fibres absorb water, they change in dimensionally (axially & transversely).
Swelling occurs in the transverse direction (width-wise) and axial direction (length-wise) of fibre. It may be expressed in terms of the increase in diameter, area, length or volume of a fibre.
The changes in dimension due to absorbing moisture or water by any textile fibre are termed as swelling properties.

## Slide 4: Swelling phenomenon of textile fibres
The molecular chains are laying roughly parallel to the fibre axis, as a result fibre has lower space between the adjacent chains and swelling will be lower.
When the fibres are immersed into water, the water molecules enter into the fibre and occupy the molecular space of fibre and thus push the fibre chains.
As a result, there will be a considerable increase in diameter of the fibre but very little increases in length.

## Slide 5: Types of Swelling
1) Transverse diameter swelling
2) Transverse area swelling
3) Axial swelling
4) Volume swelling

## Slide 6: Types of Swelling
1) Transverse diameter swelling
The fractional increase in diameter of a fibre after swelling is known as transverse diameter swelling. Transverse diameter swelling of a fibre is denoted by SD.
So, SD= ΔD/D, where ΔD= increase diameter of fibre & D= original diameter of fibre.

## Slide 7: Types of Swelling
2) Transverse area swelling
The fractional increase in area of a fibre after swelling is known as transverse area swelling. Transverse area swelling of a fibre is denoted by SA.
So, SA= ΔA/A, where ΔA= increase area of fibre & A= original area of fibre.

## Slide 8: Types of Swelling
3) Axial swelling
The fractional increase in length of a fibre after swelling is known as axial swelling. Axial swelling of a fibre is denoted by SL.
So, SL= ΔL/L, where ΔL= increase length of fibre & L= original length of fibre.

## Slide 9: Types of Swelling
4) Volume swelling
The fractional increase in volume of a fibre after swelling is known as volume swelling. Volume swelling of a fibre is denoted by SV.
So, SV= ΔV/V, where ΔV= increase volume of fibre & V= original volume of fibre

## Slide 10: Thank You

## Slide 11: Lecture 02

## Slide 12: Relation between SA & SD Relation between SA, SV and SL

## Slide 13
Transverse area swelling, SA =
Transverse dia. swelling, SD =
Volume swelling, SV =
Axial swelling, SL =

## Slide 14: Relationship between SA & SD
We know that,
Transverse area swelling, SA =
Transverse dia. swelling, SD =
For a circular fiber, area A = D2
For a swollen fiber, we get, A+∆A =
= (D2 + 2D. ∆D+∆D2)

## Slide 15: Relationship between SA & SD
Now,
SA =
=
=
=

## Slide 16: Relationship between SA & SD
=
= +
= +
= 2 SD + SD2
So, SA = 2 SD + SD2.

## Slide 17: Relationship between SA, SV and SL
We know that,
Transverse area swelling, SA = ∆A / A
Volume swelling, SV = ∆V / V
Axial swelling, SL = ∆L / L
For a circular fiber, volume, V=AL
For a swollen fiber, we get, V +∆V = (A +∆A) (L +∆L)
= AL + A∆L + ∆AL + ∆A ∆L

## Slide 18: Relationship between SA, SV and SL
Now, SV =
=
= =
= + +
= + + .
= SL + SA + SL. SA
So, SV = SL + SA + SL. SA.

## Slide 19: Thank You

## Slide 20: Lecture 03

## Slide 21: Factors influencing swelling properties of textile fibres
Composition of the material (such as cotton, polyester, acrylic, nylon etc.)
Size and form of the sample (such as fiber, yarn, fabric etc.)
External condition (temperature, humidity)
Chemical content (such as oil, wax and other impurities)

## Slide 22: Effects of swelling on textile fibres
Swelling improves the absorption of dyes and chemicals in fibre.
Due to swelling the pores of closely interlaced woven fabric will be completely blocked and thus it may act as water proof fabric.
Swelling changes the dimensional stability of fabric.
Swelling changes the electric and tensile properties of fibre.
Swelling minimizes static charge formation.

## Slide 23: Swelling (%) of different fibres:
Fibre | Transverse diameter swelling % (SD) | Transverse area swelling % (SA) | Axial swelling % (SL) | Volume swelling % (SV)
Cotton | 20 | 40 | - | -
Flax | 20 | 47 | 0.1 | -
Jute | 20 | 40 | - | -
Viscose rayon | 35 | 67 | 3.7 | 119
Wool | 14.8 | 25 | - | 37
Silk | 16.5 | 19 | 1.6 | 30
Nylon | 1.9 | 1.6 | 2.7 | 8.1

## Slide 24: Thank You